## Slide 1
Low-dispersity, high molecular weight BB peaks with high conversions
Acknowledgments
Accelerating Polymer Discovery with High-Throughput Automated Bottlebrush Block Copolymer Synthesis
Edgar Dobra, Damien Guironnet Department of Chemical and Biomolecular Engineering
What are bottlebrush block copolymers (BBCPs)?
Methods
Design of Experiments
Polymer Characterization
Polymer Synthesis
Chart: Molecular Weight (g/mol)
Gel Permeation Chromatography
GPC
Guironnet Group
Polymerizations
Results
Polymers are characterized by Gel Permeation Chromatography (GPC) based on their Molecular Weight
Developing the polymer synthesis code in Python
Designing BBCP composition
Preparing the OT-2 for inert atmosphere polymerizations
Introduction
Polymers: Large molecules composed of repeating monomer units, forming long chains1
Block Copolymers: Polymers with two or more distinct monomer blocks linked together2
Bottlebrush Polymers (BBs): Macromolecules featuring a linear backbone with densely grafted polymeric side-chains3
AUTOMATION WITH OT-2 (OPENTRONS)
A glovebox allows handling of air- or moisture-sensitive chemistry6
A liquid handler enables precise control over BBCP composition
Automated protocols facilitate conducting experiments in series efficiently
OT-2
Anionic Polymerization of Styrene
COMPARISON OF THE PS-BBs
COMPARISON OF THE PS-b-2PLAs
MAXIMUM CAPABILITIES
Similar peaks
Higher molecular weight on OT-2 can be due to slightly different loading
Future Work
STRESS TESTING SYSTEM UNDER HIGH LOADS
EXTENDING TO DIFFERENT CHEMISTRIES
OT-2
Testing system to create 50-100 different polymers simultaneously
Gram scale experiments
Produce films for photonics
Experimenting with the compatibility of the system with other air- and moisture-sensitive polymer chemistries
Extending our polymer toolbox with the help of automation
SYNTHESIS AND HIGH THROUGHPUT
BBCPs with various compositions need to be synthesized and characterized
Change in the size of the first and second block (DPPS, DPPLA)
(4) Jawiczuk, M.; Marczyk, A.; Trzaskowski, B. Decomposition of Ruthenium Olefin Metathesis Catalyst. Catalysts 2020, 10 (8), 887. | (5) Kamble, Y. L.; Shi, J.; Jeon, S.; Diao, Y.; Rogers, S.; Guironnet, D. Synthesis and Characterization of High-Density and High Degree of Polymerization Bottlebrush Block Copolymers for Photonic Applications. Macromolecules 2025, 58 (6), 3006–3015.
Goal:
  Accelerate synthesis to speed up discoveries
Problems:
  Chemistry is air- and moisture-sensitive4
  Synthesis can be complex and tedious5
Similar sharp peaks → Control experiment reproducible
Synthetic capabilities are highly dependent on what the machine does
Ability to run up to 112 reactions simultaneously
Bottlebrush block co-polymers (BBCPs)
Backbone
Brushes
Nblock1
Nbrush
Nblock2
Polystyrene block (PS)
Polylactide block (PLA)
(1) Young, R. J.; Lovell, P. A. Introduction to Polymers; CRC Press, 2011. | (2) Noshay, A.; McGrath, J. E. Block Copolymers; Elsevier, 2013. (3) Verduzco, R.; Li, X.; Pesek, S. L.; Stein, G. E. Structure, Function, Self-Assembly, and Applications of Bottlebrush Copolymers. Chemical Society Reviews 2015, 44 (8), 2405–2420.
3rd Gen. Grubbs Catalyst (G3)
DBU
Multi-Zone Stir Plate
4mL Vial Holder
Pipette Tips
Pipette
GPC Vial Holder
Glovebox w/ OT-2
2 x 100mL Beaker
400mL Beaker
96 x Pipette Tips
Multi-Zone Stir Plate
12 x 20mL Vials
28 x 4mL Vials
40 x 1.5mL GPC
15 x 15mL Falcon
6 x 50mL Falcon
Trash Container
Equipment inside OT-2
Change in the size of the brush length (DPS, DPLA)
Change the grafting density of PLA (DPn(PLA))
DPS (styrene) | 20, 30, 40
DPPS (polystyrene) | 20 → 400
DPLA (lactic acid) | 20 → 50
DPPLA (polylactic acid) | 20 → 400
DPn(PLA) (PLA chains) | 1, 2, 5
Variable Parameters
PS macromonomer in THF
G3 in Toluene
exo Norbonene n-methanol in THF
Tri(ethylene glycol) divinyl ether
DBU in THF
Lactide in THF
Boric acid in THF
PS-b-2PLA
Ring Opening Metathesis Polymerization Followed by Graft From
Data Analysis
Analyze data via Python scripts
Plot GPC graphs
Determine composition by fitting Gaussians to different polymer peaks on GPC data
Deconvolution and Analysis Using Python
Glovebox Control PS-ROMP GPC
OT-2 PS-ROMP GPC
PS Homopolymer
PS-BB
PS Homopolymer
PS-BB
 | PS-BB Control | PS-BB OT-2
Mn (g/mol) | 318000 | 333000
Đ | 1.04 | 1.05
DP | 74 | 78
Conv. (%) | 96.7 | 95.6
Experimental Data
(6) Muhr, M.; Heiß, P.; Schütz, M.; Bühler, R.; Gemel, C.; Linden, M. H.; H. Bernhard Linden; Fischer, R. A. Enabling LIFDI-MS Measurements of Highly Air Sensitive Organometallic Compounds: A Combined MS/Glovebox Technique. Dalton Transactions 2021, 50 (26), 9031–9036.
Composition based on weight* | PS Homopolymer | BB PS | Diblock PS-b-2PLA | Triblock PS-b-2PLA-b-PS
Control (%) | 4.7 | 31.0 | 44.5 | 19.8
OT-2 (%) | 9.8 | 18.1 | 51.6 | 20.4
OT-2 ROMP-GRAFT GPC
Glovebox Control ROMP-GRAFT GPC
PS Homopolymer
PS-BB
Diblock PS-b-2PLA
Triblock PS-b-2PLA-b-PS
PS Homopolymer
PS-BB
Diblock PS-b-2PLA
Triblock PS-b-2PLA-b-PS
Calculated Composition Data
Successful automation of BBCP synthesis
*Assuming polymers have similar sample constants for GPC intensity
With precipitation and GPC ✔
45 x 200mg (5g) polymer, precipitation in 15mL Falcon (3x excess)
18 x 200mg (3.6g) polymer, precipitation in 50mL Falcon (15x excess)
96 x Pipette Tips
Trash Container
80 x 1.5mL GPC
45 x 15mL Falcon
2 x 100mL Beaker
56 x 4mL Vials
12 x 20mL Vials
400mL Beaker
192 x Pipette Tips
Trash Container
12 x 20mL Vials
112 x 4mL Vials
400mL Beaker
6 x 100mL Beaker
Without precipitation nor GPC ✘
112 x 200mg (22.4g) polymer, reaction in 4mL Vials
48 x 1g (3.6g) polymer, reaction in 20mL Vials
Dried out BBCP
Films with BBCP photonics